BS4360 WR 50 B; WR 50 B steel plate; WR 50 B steel sheet; WR 50 B steel grade; WR 50 B steel supplier

- WR 50 B steel description

WR 50 B steel is a weather resistant steel which could more accurately be termed as an "Atmospheric Corrosion Resistant Steel" and often referred to as Corten-B steel. Weathering means that due to WR 50 B steel chemical compositions, WR 50 B steel chemical composition can increase resistance to atmospheric corrosion compared to unalloyed steels. This is because it forms a protective layer on WR 50 B steel surface under the influence of the weather.

- WR 50 B steel Application range

Due to the WR 50 B steel super property as main weathering steel, WR 50 B steel has a widely use in Mine fans, earth moving buckets, trailers and large road vehicles, drill rings, cranes, excavators, underground mining equipment, bridges and other high strength components requiring superior toughness.

- WR 50 B steel supply size

Thickness: 2mm to 460mm

Width: 1500mm to 3200mm

Length: 6000mm to 12000mm

(other plate sizes and thicknesses available on request )

- WR 50 B steel Deliver condition

Hot Rolled, Cold Rolled, Normalized, Quenched, Tempering, Thermal Mechanical Control Process (TMCP), Electroslag Remelting Technical, HIC test.

5. WR 50 B steel Chemical composition(% )

| C. | Mn. | Si. | S. | P. | Nb. | V. |
| --- | --- | --- | --- | --- | --- | --- |
| 0.20 | 1.5 | 0.5 | 0.05 | 0.05 | 0.003 / 0.1 | 0.003 / 0.1 |

- WR 50 B steel mechanical property

| Normal Thickness (mm) | Tensile Strength (MPa) | Min. Yield Strength (MPa) | % Elong in 200 mm (Min) | Impact Strength J (Min) |
| --- | --- | --- | --- | --- |
| 5 - 150 | 490 - 640 | 305 - 355 (Depends on thickness) | 18 | Not specified or measured |

Henan BEBON international co.,ltd is an outstanding and professional WR 50 B steel exporter and stockist in china, especially in super thick atmospheric corrosion resistance of structural steel plate. We keep more than 10000 ton WR 50 B steel in stock, and we have a good relationship with per big steel mill, so if you have any WR 50 B steel need, we also can meet your maximum request. To choose the reliable and best supplier, BEBON international is your best choice. Any need in WR 50 B steel, we can supply you with the best quality, best service and competitive price.