BS 4360 WR 50 C; WR 50 C steel; WR 50 C steel plate; WR 50 C steel grade; WR 50 C steel supplier

- WR 50 C steel description

As a structural weathering steel, WR 50 C steels have a super property. WR 50 C steel chemical composition can increase resistance to atmospheric corrosion compared to other steels. This is because it forms a protective layer on WR 50 C steel surface under the influence of the weather.

- WR 50 C steel Application range

WR 50 C steel weathering steel has a widely use in Mine fans, earth moving buckets, trailers and large road vehicles, drill rings, cranes, excavators, underground mining equipment, bridges and other high strength components requiring superior toughness.

- WR 50 C steel supply size

Thickness: 2mm to 460mm

Width: 1500mm to 3200mm

Length: 6000mm to 12000mm

(other plate sizes and thicknesses available on request )

4. WR 50 C steel deliver condition

Hot Rolled, Cold Rolled, Normalized, Quenched, Tempering, Thermal Mechanical Control Process (TMCP), Electroslag Remelting Technical, HIC test.

5. WR 50 C steel chemical composition(%)

| C | Si | Mn | P | S | Cu | Cr | Ni | V | Nb | Al |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Max 0.16 | Max 0.50 | Max 0.50-1.50 | Max 0.035 | Max 0.035 | Max 0.25-0.55 | Max 0.40-0.80 | Max 0.65 | Max 0.02-0.12 | Max 0.015-0.060 | Min 0.02 |

- WR 50 C steel mechanical property

| Thickness | Yield Strength ReH[N/mm2] transv.min | Tensile Strength Rm[N/mm2]transv | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| ---- | 355 | 510-610 | 22 | ---- |

As an outstanding exporter and stockist in china, especially in Atmospheric Corrosion Resistant Steel, Henan BEBON international co.,ltd enjoy a famous reputation in the global steel market. Due to we have a good and close relationship with per big steel mill, so if you have any need about WR 50 C steel, we all can make you satisfied with our weathering steel. In addition, we have WR 50 C steel more than 10000 tons per mouth in stock, so if you need. Pls don't hesitate to contact BEBON sales-team now.