S355K2G2W steel plate,weathering steel S355K2G2W supplier,corrosion resistant/weather resistant steel S355K2G2W,EN10155  S355K2G2W steel sheet.

EN 10155  S355K2G2W  weathering steel MATERIAL#1.8967 S355K2G2W

S355K2G2W Weathering Steel Description:

"Weathering" means that due to the chemical compositions of S355K2G2W, these steel plates and sheets exhibit increased resistance to atmospheric corrosion compared to other steels.

S355K2G2W corrosion resistant steel is of EN 10155 standard,S355K2G2W material number is 1.8967,S355 K2G2W steel plates have equality material in WBL 087,ASTM ,NFA 35502,BS4360,CSA G 4021 standard.

S355K2G2W Weathering Steel Delivery Conditions:

Hot rolled,Normalization,Tempering,Quenched,Normalization and Tempering,Quenched and Tempering,UT,PWHT,IMPACT TEST,Thermal Mechanical Control Process (TMCP),Electroslag Remelting Technical,HIC test,etc

S355K2G2W Weathering Steel Applications:

S355K2G2W weathering steel is popularly used in outdoor sculptures,bridge and other large structural applications, marine transportation, in the construction of Intermodal containers.S355K2G2W steel is used for various types of welded, bolted and riveted constructions e.g. steel frame structures, bridges, tanks and containers, exhaust systems, vehicles and equipment constructions.

S355K2G2W Weathering Steel Chemical Composition:

| Steel Grades | C max | Si max | Mn | P max | S max | Cu max | Cr max | Ni max | Mo max |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S355K2G2W | 0.16 | 0.50 | 0.50-1.50 | 0.035 | 0.035 | 0.25-0.55 | 0.40-0.80 | 0.65 | - |

S355K2G2W Weathering Steel Mechanical properties：

| Thickness | Yield Strength ReH[N/mm2]transv.min | Tensile Strength Rm[N/mm2]transv | Fracture Elongation[%]transv. min. | Notch ImpactEnergy1)Ch Vcomplete samplelongitud. min [J] |  |
| --- | --- | --- | --- | --- | --- |
| - | 315 - 355 | 490 – 680 | - | - | - |

S355K2G2W Weathering Steel Services:

Pretreatment(Derusting,Lacquering,Painting,Sand Clusting),Heat treatment,UT Test,HIC Test,Impact Test,PWHT Z15 Test, Z25 Test, Z35Test,Cutting, Welding ,Inspection from the third party like SGS,Galvanization.

EN 10155 S355K2G2W steel plate/weathering steel/corrosion resistant/weather resistant steel: BEBON can supply the stock steel grade S355K2G2W Weathering Steel,BEBON International is a professional S355K2G2W steel plates exporter,supplier,manufacturer and stockist in China.Any need in S355K2G2W Weathering Steel,please feel free to contact us!we will offer you the most competitive price of S355K2G2W and best service for S355K2G2W.