SEW 087 WTSt 52-3; WTSt 52-3 steel; WTStT52-3 steel plate; WTSt 52-3 steel grade; WTSt 52-3 steel supplier

1. WTST 52-3 steel description

WTST 52-3 steel is a structural weathering steel which is also referred to as atmospheric corrosion resistant steel.

WTST 52-3 steels have a super property. WTST 52-3 steel chemical composition can increase resistance to atmospheric corrosion compared to other steels. This is because it forms a protective layer on WTST 52-3 steel surface under the influence of the weather.

- WTST 52-3 steel Application range

Due to the super property of WTSt 52-3 steel, WTSt 52-3 steel has a widely use in Mine fans, earth moving buckets, trailers and large road vehicles, drill rings, cranes, excavators, underground mining equipment, bridges and other high strength components requiring superior toughness.

- WTSt 52-3 steel supply size

Thickness: 2mm to 460mm

Width: 1500mm to 3200mm

Length: 6000mm to 12000mm

(other plate sizes and thicknesses available on request )

- WTSt 52-3 steel deliver condition

Hot Rolled, Cold Rolled, Normalized, Quenched, Tempering, Thermal Mechanical Control Process (TMCP), Electroslag Remelting Technical, HIC test.

- WTSt 52-3 steel chemical composition(%)

| C | Si | Mn | P | S | Cu | Cr | Ni | V | Nb | Al |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Max 0.16 | Max 0.50 | Max 0.50-1.50 | Max 0.035 | Max 0.035 | Max 0.25-0.55 | Max 0.40-0.80 | Max 0.65 | Max 0.02-0.12 | Max 0.015-0.060 | Min 0.02 |

- WTSt 52-3 steel mechanical property

| Thickness | Yield Strength ReH[N/mm2] transv.min | Tensile Strength Rm[N/mm2]transv | Fracture Elongation[%]transv. min. | Notch Impact Energy1)Ch Vcomplete samplelongitud. min [J] |
| --- | --- | --- | --- | --- |
| ---- | 355 | 510-610 | 22 | ---- |

As an outstanding exporter and stockist in china, especially in Atmospheric Corrosion Resistant Steel, Henan BEBON international co.,ltd enjoy a famous reputation in the global steel market. Due to we have a good and close relationship with per big steel mill, so if you have any need about WTSt 52-3 steel, we all can make you satisfied with our weathering steel. In addition, we have WTSt 52-3 steel more than 10000 tons per mouth in stock, so if you need. Pls don't hesitate to contact BEBON sales-team now.