UNI Fe 510 C2K1; Fe 510 C2K1 steel; Fe 510 C2K1 steel plate; Fe 510 C2K1 steel grade; Fe 510 C2K1 steel supplier

- Fe 510 C2K1 steel description

As a structural weathering steel, Fe 510 C2K1 steels have a super property. Fe 510 C2K1 steel chemical composition can increase resistance to atmospheric corrosion compared to other steels. This is because it forms a protective layer on Fe 510 C2K1 steel surface under the influence of the weather.

- Fe 510 C2K1 steel Application range: Fe 510 C2K1 steel steel is used for various types of welded, bolted and riveted constructions e.g. steel frame structures, bridges, tanks and containers, exhaust systems, vehicles and equipment constructions.

- Fe 510 C2K1 steel supply size

Thickness:2mm to 460mm

Width: 1500mm to 3200mm

Length: 6000mm to 12000mm

(other plate sizes and thicknesses available on request )

- Fe 510 C2K1 steel deliver condition

Hot Rolled, Cold Rolled, Normalized, Quenched, Tempering, Thermal Mechanical Control Process (TMCP), Electroslag Remelting Technical, HIC test.

- Fe 510 C2K1 steel chemical composition(%)

| C | Si | Mn | P | S | Cr | N | Cu | CEV |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| max 0.16 | Max 0.5 | 0.5 - 1.5 | max 0.035 | Max 0.035 | 0.4 -0.8 | max 0.009 | 0.25-0.55 | Max 0.52 |
| Note: 1. The steels may show a Ni content of max 0.65 %; 2. For long Fe 510 C2K1 steel, the P and S content can be 0.005% higher; 3. The Fe 510 C2K1 steel may contain max. 0.30 % Mo and max. 0.15 % Zr 4. It is permissible to exceed the specified values provided that for each increase of 0.001 % N, the P max. content will be reduced by 0.005 %; the N content of the ladle analysis, however, shall not be more than 0.012 % 5.The max. value for nitrogen does not apply if the chemical composition shows a minimum total Al content of 0.020 % or if sufficient other N binding elements are present. |  |  |  |  |  |  |  |  |

6. Fe 510 C2K1 steel mechanical property

| Nominal thickness (mm) | to 16 | 16-40 | 40-63 | 63-80 | 80-100 | 100-150 |
| --- | --- | --- | --- | --- | --- | --- |
| ReH - Minimum yield strength (MPa) | 355 | 345 | 335 | 325 | 315 | 295 |
| Nominal thickness (mm) | To 3 |  | 3-100 |  | 100-150 |  |
| Rm -Tensile strength (MPa) | 510-680 |  | 470-630 |  | 450-600 |  |
| Nominal thickness (mm) | 3-40 |  | 40-63 |  | 63-100 | 100-150 |
| A - Minimum elongation Lo = 5,65 √ So (%) | 22 |  | 21 |  | 20 | 18 |
| Nominal thickness (mm) | 1.5 - 2 |  | 2-2.5 |  | 2.5-3 |  |
| A - Minimum elongation Lo = Lo = 80 mm (%) | 16 |  | 17 |  | 18 |  |
| Temperature | -20 |  |  | 0 |  |  |
| Notch impact test. Min. absorbed energy | 27 |  |  | 27 |  |  |

Henan BEBON international is an outstanding exporter and stockist in china, especially in Atmospheric Corrosion Resistant Steel, also named weathering steel. As our have a good relationship with per big steel mill, so we have Fe 510 C2K1 steel more than 10000 tons in stock. If you any need about Fe 510 C2K1 steel , whatever the specification, we also can meet your maximum request. More technology information, welcome to freely contact BEBON sales-team.